# 5311AS	ASONA TILE PERFORATED CEILING TILES

This section deals with the manufacture, supply and installation of Asona ceiling systems, including associated acoustical wall elements offered by Asona Limited to complete the system.

GUIDANCE NOTE

Check the manufacturer’s data sheets and modify this section accordingly.

## 1.	GENERAL

GUIDANCE NOTE

Masterspec does not recommend the use of SCOPE or SCOPE OF WORK clauses.  However there are some forms of contract where a general description of what is covered by a particular work section can help guide those using the specification.  If you prefer to include such a general description, add it directly underneath the work section title, not as a numbered clause.

Related work

### 1.1	RELATED SECTIONS

Refer to ~ for ~.

GUIDANCE NOTE

Include cross references to other sections where these contain related work.

Documents

### 1.2	DOCUMENTS

Documents referred to in this section are:

NZS 1170	Structural design actions, Earthquake actions – New Zealand

ISO 5660.1 	Cone calorimeter test reaction to fire tests for heat release, smoke production and mass loss rate.

NZBC C/AS1	Fire Safety

AS/NZS 2785	Suspended ceilings - Design and installation

AS 2946	Suspended ceilings, recessed luminaries and air diffusers - Interface requirements for physical compatibility

NZS 4219	Seismic resistance of engineering systems in buildings

ISO 354	Test method for sound absorption by reverberant room method

ISO 11654	Weighted sound absorption ratings

ASTM C423	Test method for sound absorption and sound absorption coefficients by the reverberation room method

Documents listed above and cited in the clauses that follow are part of this specification.  However, this specification takes precedence in the event of it being at variance with the cited document.

GUIDANCE NOTE

Delete from the DOCUMENTS clause any document not cited.  List any additional cited documents.

RELATED DOCUMENTS

Refer to the following related documents when preparing this section:

ISO 11654	Ratings standard for sound absprption

BRANZ Bulletin 369: Fitting tolerances

### 1.3	MANUFACTURER’S DOCUMENTS

Manufacturer’s and supplier’s documents relating to work in this section are:

Asona data sheets for

Asona Tile, round hole or slot perforated timber panel

Copies of the above literature are available online at www.asona.co.nz .

For lead times and pricing contact Asona Ltd, Unit 14, 7 Cain Road, Penrose, Auckland.

Email:	info@asona.co.nz

Telephone:	09 525 6575

GUIDANCE NOTE

It is important to ensure that all personnel on site have access to accurate, up to date technical information on the many products, materials and equipment used on a project.  In most cases individual products are not used in isolation, but form part of a building process.  Also a particular manufacturer’s and/or supplier’s requirements for handling, storage, preparation, installation, finishing and protection of their product can vary from what might be considered the norm.  Access to technical information can help overcome this potential problem.

Requirements

### 1.4	SAMPLE SECTION

Allow to erect a sample section of the suspended ceiling system offered.  Subject to confirmation in writing, the sample section may form part of the completed installation.

Refer to 4. SELECTIONS for location.

GUIDANCE NOTE

Amend or expand this clause as appropriate to the project, including requirements for incorporating other elements - luminaires, diffusers, surrounding surfaces - into the sample section.

### 1.5	INSTALLATION

Minimum installation standard to AS/NZS 2785 and ASTM C636.  Installation to be only by the manufacturer’s accredited installer, using the manufacturer’s technical services.  Accredited installers to be members of the Association of Wall and Ceiling Industries of New Zealand (AWCI) Provide evidence of experience, listing completed projects of similar size and complexity.

### 1.6	CLEANING

Clean using soft bristled brush, vacuum or a damp cloth or as noted in product data sheet.

### 1.7	SPARES

Provide spare matching ceiling elements in the quantities specified below.  Deliver into a dry store at the site or elsewhere as directed and at agreed times.  Refer to 4. SELECTIONS for quantity.

GUIDANCE NOTE

Ask for packs of tiles.

### 1.8	SUPPLY WARRANTY

Supply a manufacturers 5 year warranty against manufacturing defects and durability compliance per NZBC B2 of 5 years for accessible tiles and 15 years for suspension components.

1.9	NO SUBSTITUTIONS

Substitutions are not permitted to any specified Asona system, or associated components and products.

Performance

GUIDANCE NOTE

Use these clauses if specifying by performance.

NOTE: Even when specifying by brand it may still be necessary to include some reference to performance.

### 1.10	LOADING CODE REQUIREMENT

Comply with the requirements of NZS 1170, section 8.

### 1.11	CERTIFICATION

Provide:

-  NZS 1170, section 8 for evaluation

-	certificates and other evidence that the system offered complies with the standards of performance specified

-	a Producer Statement on completion.

### 1.12	ACOUSTIC REQUIREMENTS

Verify material sound absorption performance. Submit a copy of a full scale sound absorption test report to ISO 354 E200 as tested by Auckland Uni Services or other independent testing authority.  Refer to 4. SELECTIONS for acoustic performance requirements.

### 1.13	REACTION TO FIRE PROPERTIES

Reaction to fire properties of the wall / ceiling finishes must meet the acceptable solutions to all risk groups C/AS1 to C/AS7. Risk groups: SH,SM,SI,CA,WB,WS,VP

ASONA PRODUCT FIRE GROUP NUMBER RATINGS

5660-1 Cone Calorimeter test

| ASONA PRODUCTS | 12mm Fire Rated MDF | Standard MDF | Plywood |
| --- | --- | --- | --- |
| Atkar | Veneer | Melamine | Veneer/ Polyurethane | Paint | ~ | ~ |
| Asona Slat | 1S | 1S | 2 | 1S | 3 | 3 |
| Asona Slot | 1S | 1S | 2 | 1S | 3 | 3 |
| Asona Tile | 1S | 1S | 2 | 1S | 3 | 3 |
| Asona Panel | 1S | 1S | 2 | 1S | 3 | 3 |

GUIDANCE NOTE

Key criteria are spread of flame and smoke developed indices. consult your fire engineer for advice.

### 1.14	ENVIRONMENTAL REQUIREMENTS

Design the ceiling system for use over its expected life without deterioration within the required temperature and humidity range.  Refer to 4. SELECTIONS for details.

GUIDANCE NOTE

If this clause is not used and the SITE CONDITIONS clause cannot be complied with, then allowance needs to be made for a tile and sheet linings that will not sag over the construction period.

### 1.15	LIGHT REFLECTANCE

To ASTM C1477.  Refer to 4 SELECTIONS for reflectance and colour.

GUIDANCE NOTE

Data from selected product technical data sheet

## 2.	PRODUCTS

GUIDANCE NOTE

Select the proprietary system to suit the brief.  Use the PRODUCTS clauses to get the desired finish and required fire and acoustic characteristics.  Use the EXECUTION clauses required for the selected system.

Materials – Accessible grid and tile ceiling systems

### 2.1	PERFORATED TIMBER PANELS

Asona Tile™ round hole or slot perforated MDF or ply panels as selected with pre finished timber grain and decorative surfaces, IAB acoustic tissue backer and edge profiled.

### 2.2	GRID SUSPENSION SYSTEM

Supplied by Asona Ltd Tel: 09 525 6575

Type: Hot dip galvanized steel elements to ASTM C635 intermediate duty for carrying ceiling panels, light fixtures and air distribution elements and complying with NZS 1170, section 8.

GUIDANCE NOTE

Check the supplier’s data sheets and expand this clause to describe project requirements.

## 3.	EXECUTION

Conditions

### 3.1	CO-ORDINATE SERVICES

Co-ordinate and co-operate with electrical and mechanical work to avoid conflict between framing members and luminaires, diffusers, pipework and ducting.  Confirm the provision of extra support and fixings.

### 3.2	SITE CONDITIONS

Do not begin installation until the building is closed in, fully glazed, the roof watertight, and mechanical and electrical duct work above the ceiling completed.

### 3.3	COMPLY

Comply with AS 2946 for interface requirements for physical compatibility.

### 3.4	RESPONSIBILITY

Ensure that conditions are suitable for the ceiling installation. Arrange for the programming of the work to suit required practice.

Application

### 3.5	INSTALL

Install the system to AS/NZS 2785 minimum standards and the ceiling manufacturer's requirements.

### 3.6	ACCESSIBILITY

Provide access to the ceiling system and the in-ceiling and above-ceiling services so that maintenance and removal of any part can be carried out without damage to the ceiling system or panels.

GUIDANCE NOTE

As full access in all areas is clearly impractical, any special requirements for clear access will need to be defined; either by description here, or on the drawings.

### 3.7	PENETRATIONS

Accommodate recessed light fittings, air conditioning outlets and other electrical and/or mechanical services that are fixed to or pass through the ceiling system. Provide independent support for these as necessary. Such fittings are not to be supported by the acoustical ceiling panels.

### 3.08	PROTECT EXISTING WORK

Protect adjacent existing work from damage during the installation.

Completion

### 3.09	REPLACE

Replace or repair damaged or marked elements.  Recycle material, consult manufacturer for replacement facers or painting procedure.

### 3.10	LEAVE

Leave work to the standard required by following procedures.

### 3.11	REMOVE

Remove debris, unused elements and elements from the site.

### 3.12	CLEAN

Clean soiled or marked units.

## 4.	SELECTIONS

Requirements

### 4.1	SAMPLE SECTION

Location:	~

Size: 	~ m x ~ m

Performance

### ACOUSTIC REQUIREMENTS

Practical sound absorption properties per ISO 354 E200, ratings per ISO 11654

| Frequency | 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz |
| --- | --- | --- | --- | --- | --- | --- |
| (P | ~ | ~ | ~ | ~ | ~ | ~ |

Sound absorption class:		A

Weighted sound absorption coefficient (W:	~ minimum

NRC per ASTM C423-99:		~ minimum

GUIDANCE NOTE

Specify individual frequency Hz for best results, acoustic data available from selected product technical data sheet or acoustical test report

### 4.3	ENVIRONMENTAL REQUIREMENTS

Range:	10 - 30°C

Relative humidity:	90 % maximum

### 4.4	REFLECTANCE

Reflectance:	(~)

For (colour):	(~)

For other colours:	(~)

4.5	FIRE

Group Number: 1S (F/R MDF with Paint, Melamine, Veneer)

2   (F/R MDF Veneer + Polyurethane)

3   (Standard MDF / Ply)

GUIDANCE NOTE

If this clause is not used and the SITE CONDITIONS clause cannot be complied with, then allowance needs to be made for a tile that will not sag over the construction period.

### 4.6	SCHEDULE

| Area | Product Ref. | Perforation |
| --- | --- | --- |
| ~ | Asona Tile | (as selected) |

GUIDANCE NOTE

Identify areas and note product type, finish and acoustical ratings required.

Accessible panel with suspended grid systems

### 4.7	CEILING PANEL

Brand/product:	Asona Tile™ (Meteor slot perforated)(Constellation 4mm Ø round perforation)(Galaxy 10mm Ø round perforation) as supplied by Asona Ltd,

Tel: 09 525 6575, fax: 09 525 6579, email: info@asona.co.nz

Material Type:	MDF (Fire Rated MDF)

Thickness:	12mm

Size: 	(600 x 600 mm)(1200 x 600 mm

Finish: 	Veneer as selected

Colour: 	as selected

GUIDANCE NOTE

Product:

Atkar brand perforated timber panels - Au.diTile™ round hole or slot perforated MDF or ply lay in ceiling panels with pre finished timber grain and decorative surfaces, IAB acoustic tissue backer and edge profiled to suit T24 or T15 exposed grid systems. Imported, lead times 6-7 weeks

Type:

Meteor	Slot perforated 13.3 % open area

Constellation	Round perforated 10.2 % open area

Galaxy	Round perforated 12.5 % open area

Confirm the compatibility of recessed lighting, air conditioning unit and ventilation outlets to the ceiling grid.

### 4.8	SUSPENSION GRID

Type:	Asona (T15)(T24)

Material: 	Galvanised steel

Finish/colour: 	(white) (other)

Module: 	to suit tile

Hanger:	2.5mm wire at 1200 mm centres

GUIDANCE NOTE

Type:

T15 	15 mm faced exposed grid with  white paint coating to face

T24 	24 mm faced exposed grid, white paint coated, economical

Hanger:	Standard 2.5 mm hanger wire fixed to grid

Option of  direct fix CL070 clip, face of ceiling 80 mm from soffit.

### 4.9	PERIMETER TRIM

Type:	~

Material:	~

Finish/colour:	~

GUIDANCE NOTE

Type:

WA2022	20 mm x 22 mm wall angle, white paint coated galvanized steel body

WA2040	20 mm x 40 mm wall angle, white paint coated galvanized steel body

WAS1010	Shadowline wall angle, 10 mm x 10 mm negative, white coated steel body

### 4.10	ACCESS HATCHES

Type:	~

Material:	~

Finish/colour:	~

Size:	~ mm x ~ mm

GUIDANCE NOTE

Access hatches may be require to access M/E services in plenum, size according to need..

Spares

### 4.11	SPARES

Panels:	~

GUIDANCE NOTE

Ask for full panels.